Investigation of the thermal management potential of phase change material for lithium-ion battery

Haocheng Wang a #, Yanhong Guo a, b #, Yong Ren a, b, c, d *, Siegfried Yeboah e, Jing Wang c, f, Fei Long a, b, g, Zhiyu Zhang a, b, c, Rui Jiang a, h

a Department of Mechanical, Materials and Manufacturing Engineering, University of Nottingham Ningbo China, Ningbo, China

b Research Group for Fluids and Thermal Engineering, University of Nottingham Ningbo China, Ningbo, China

c Nottingham Ningbo China Beacons of Excellence Research and Innovation Institute, Ningbo, China

d Key Laboratory of Carbonaceous Wastes Processing and Process Intensification Research of Zhejiang Province, University of Nottingham Ningbo China, Ningbo, China

e School of the Built Environment and Architecture, London South Bank University, London, United Kingdom

f Department of Electrical and Electronic Engineering, University of Nottingham Ningbo China, Ningbo, China

g Key Laboratory of Additive Manufacturing Materials of Zhejiang Province, Ningbo Institute of Materials Technology and Engineering, Chinese Academy of Science, Ningbo, China

h Advanced Intelligent Manufacturing Research Group, University of Nottingham Ningbo China, Ningbo, China

*Corresponding authors: yong.ren@nottingham.edu.cn

# These authors contributed equally to the paper

Abstract

With the rapid development of electric vehicles, lithium-ion batteries have been widely used as an energy source. However, to avoid thermal runaway and to ensure the correct operation of lithium-ion battery system, effective battery thermal management would be required. In this study the capacity of seven phase change materials to respectively manage thermal issues associated with lithium-ion battery is theoretically investigated using computational fluid dynamics. The impacts of shell material, heat transfer coefficient, phase change material fill volume and shape of the battery pack on the thermal performance of the lithium-ion battery/phase change material (LIB/PCM) system are investigated. The results show that when the ambient temperature was 20°C or 30°C, phase change material-RT35 showed the best temperature control ability for the system, while phase change material-RT50 had better thermal management capability when the ambient temperature was 40°C. Also, shell material with higher thermal conductivity or heat transfer coefficient increase, effectively reduced the maximum temperature of the lithium-ion battery and the temperature difference within the proposed system. The phase transition time in the LIB/PCM system with a heat transfer coefficient of 10 W/m2K was nearly four times longer compared to that of 1 W/m²K. Here, the maximum temperature attained after 150 minutes of charging and discharging was 55.18 °C, around 62.30% cooler than at 1 W/m²K. It was also observed that larger phase change material (PCM) volume ratio led to lower system temperature during phase transition. The continuous charging and discharging after complete transformation of the phase change material was found to impact negatively on the thermal management of the lithium-ion battery system. The shape of the lithium-ion battery system was also found to influence thermal management of the lithium-ion battery irrespective of having the same volume of PCM in the battery pack. After 150 minutes of charging and discharging, the rectangular shaped LIB/PCM system with similar PCM fill volume was found to surpass the circular one by 14.78°C in maximum temperature, while attaining a minimum temperature difference of 9.6°C.

Keywords: Phase change material, Lithium-ion battery, Thermal management system, Parameter study, Optimized battery arrangement

1. Introduction

Rapid industrial development and growth of the world’s population since the industrial revolution has led to significant global energy consumption, environmental pollution, increase in carbon emissions, and other related problems [1]. The global transport sector for instance, consumes significant amounts of fossil fuel energy and takes up about 49% of fossil fuel-based resources hence has attracted the attention of local governments [2]. With many countries focused on improving their environment, attention is now on where possible moving away from fossil fuel-based sources or optimizing their utilization efficiency. Here, electric vehicles (EVs) and hybrid electric vehicles (HEVs) using electricity as the main driving energy instead of conventional fossil fuels are being rapidly developed to achieve that towards minimizing carbon emissions [3-6]. According to Andersen et al. [7] nations could reduce their greenhouse gas emissions by 20% by transitioning to EVs, with a further 40% emissions reduction possible if the electricity for the EVs is generated from renewable energy. When it comes to EVs, lithium-ion batteries (LIBs) are the main energy source. Compared to alternatives like lead-acid and nickel-metal hydride batteries, lithium-ion batteries (LIBs) have long life cycle, better efficiency, high energy and power density [8-11]. However, they also have associated limitations such as overheating and safety related issues [5]. For instance, Li et al. [12] found that LIBs are very sensitive to operating temperature as the battery pack with a shell is more difficult to control when thermal runaway occurs than the battery pack without a shell. During charging and discharging, chemical reactions inside the battery generate significant amounts of heat which influences their performance [13]. Several studies [14-16] have shown that if this heat is not effectively removed, the temperature of the LIBs increase rapidly leading to thermal runaway and catastrophic damage, especially when in a battery pack consisting of multiple cells. Experimental work by Zhao et al. [17] shows that, when a 1.2 Ah LIB experiences thermal runaway, its internal temperature could rise from about 25 °C to more than 100 °C in just 70 seconds. Also, the temperature difference between each cell in the battery pack can lead to premature failure of the battery pack, or even explosion [18]. For typical LIBs, the optimal operating temperature range is between 20°C to 40°C. Under moderate load, the maximum temperature of the battery should not exceed 50°C. Too high or too low working temperature greatly reduces working efficiency, and can lead to heat runaway, serious safety issues and the release of high temperature harmful gases containing large amounts of CO, H2, and CO2 [19-22]. For this reason, evaluating the performance of LIB under various conditions using criteria such as maximum temperature and temperature difference has become a very valuable research direction [23, 24].

To ensure the safety and efficiency of the battery module in practical applications, battery systems and grid storage of EVs and HEVs normally consist of a large number of batteries to meet voltage and capacity requirements and are usually related to a battery thermal management system (BTMS) [25]. BTMS is mainly divided into air cooling, liquid cooling, and phase change cooling [17]. Air cooling has a simple structure and can directly reduce the external temperature of the battery pack [26]. However, on temperature rise above 66 °C, cooling the battery to below 52°C using this approach becomes a challenge. For instance, when the battery pack is heavily loaded at ambient temperatures higher than 40 °C, the temperature distribution inside the battery pack becomes uneven limiting the capacity of air cooling in overcoming thermal runaway phenomenon [23, 27]. Liquid-based cooling strategy on the other hand provides a better cooling option for EVs in high temperature environments due to the relatively high thermal conductivity of liquids compared to air cooling technique. It can be divided into direct/immersive liquid cooling which involves a cooling fluid in direct contact with the battery, and indirect liquid cooling which involves the injection of coolant into the cooling plate or riser to cool the battery. Leakage and efficiency however are the key limitations for the direct/immersive liquid cooling approach, while for indirect liquid cooling, the complex structure and uneven temperature distribution are the main drawbacks [28-32]. In terms of solid to liquid phase change cooling, the rise in temperature of the battery pack during operation creates a temperature difference between the battery pack and the phase change material (PCM). The heat generated by the battery pack is absorbed by the solid PCM leading to phase transition from solid to liquid. During this phase transition, the temperature of the PCM remains almost constant, which limits the increase in cell temperature [33, 34]. This passive cooling approach has relatively small volume and high cooling efficiency unlike liquid cooling where a pump may be required [25, 35, 36]. Therefore, compared to air and liquid cooling, phase change cooling has greater potential in the application of BTMS [22, 35-39]. By changing the thickness of the PCM surrounding the LIB, Weng et al. [40] optimized the cooling effect of a BTMS. Sun et al. [41] added fins to PCM based BTMS, thereby improving the thermal conductivity of the PCM. Wang et al. [8] optimized the temperature control and service life of a BTMS by using three different PCMs comprising pure paraffin (PCM 1), composite made of 20% expanded graphite (EG), 80% paraffin (PCM 2), and composite made of 3% EG, 47% epoxy, 50% paraffin (PCM 3) respectively. In their study, the temperature difference, ∆T, of the experimental group with PCM 2 reduced by 20% at a charge-discharge rate of 5C compared to the experimental group with PCM 1. They found that composite material offers a promising solution for controlling the temperature of the battery modules and reducing temperature differences. Mohammed et al. [42] studied the cooling performance and temperature uniformity of battery thermal management systems under various PCM configurations. They found that increasing the intake speed had a smaller inhibitory effect on the temperature rise in the early discharge stage, but the effect improved as the discharge time extended to 3600s. He et al. [43] conducted an optimization study on low-temperature preheating strategy of LIBs using supercooling phase change material, based on response surface methodology. They found that an increase in PCM thickness reduced preheating time and temperature difference, however, it also led to an increase in the battery temperature and mass energy density.

Based on the literature surveyed, it was found that the use of PCM can improve the thermal performance of LIB system. However, the influence of some important parameters such as shell material and the shape of the battery packs on the performance of LIB/PCM system is still lacking. Besides, previous studies [8, 40-43] only focused on the performance of LIB/PCM systems during phase transition, with little consideration given to the impact of PCM on LIB system performance after the phase transition process is completed, which should be considered in practical applications. To fill this research gap, in this numerical study, seven PCMs with different thermophysical properties were used to explore their thermal management potential for LIB system. The effects of PCM with different melting point temperature on the thermal control capacity of LIB/PCM system during a relatively long charging and discharging time under different ambient temperature were evaluated. On this basis, the impacts of shell material, heat transfer coefficient, PCM volume ratio and the shape of the battery pack on the thermal performance of the LIB/PCM system were explored in detail using ANSYS 2022 R2 commercial CFD software.

2. Problem Description

Referring to Patel et al. [33] and Choudhari et al. [44], the lithium-ion battery (LIB) used in this study was NCR18650PF (Panasonic). The 18 in the battery name refers to battery diameter of 18 mm, the 65 refers to battery height of 65 mm and the 0 before the letter P refers to the cylindrical shape of the battery. The material of the cathode and anode of the LIB is LiFePO4 and graphite respectively. The nominal voltage and nominal capacity of the battery was 3.6 V and 2.4 Ah respectively. Table 1 shows the specifications of NCR18650PF LIB provided by the battery manufacturer and Figure 1 shows the 3D model of the main battery pack containing 16 LIBs.

Table 1. Specifications of NCR18650PF lithium-ion battery*.

| Property | Specification |
| --- | --- |
| Dimension (mm) | 18 × 65 |
| Density (kg/m3) | 2720 |
| Heat capacity (J/kg∙K) | 300 |
| Thermal conductivity (W/m∙K) | 3 |
| Nominal voltage (V) | 3.6 |
| Nominal capacity (Ah) | 2.4 |
| Internal resistance (mΩ) | 30 |

* Provided by the battery manufacturer.

Figure 1. 3D model of the LIB/PCM system.

Battery arrangement and shape affects the surface area of the LIB/PCM unit in contact with the ambient, thereby influencing the thermal management capability of the entire system. Hence, in this study, the LIB/PCM units with square, circular, and rectangular configurations having corresponding lateral areas of 22620 mm2, 20012 mm2 and 23140 mm2 respectively with almost the same volume (the model with the largest volume was 0.74% larger than the model with the smallest volume) was used (See Figure 2).

Figure 2. Configurations of LIB/PCM system (a) Square (b) Circular (c) Rectangular.

Different PCMs have different thermophysical properties, therefore choosing an appropriate one has great significance on the thermal performance of the LIB/PCM system. Theoretically, PCMs with higher latent heat capacity absorb more heat during the phase change process and can control the temperature of the LIB pack much more effectively. The PCM melting temperature on the other hand determines the working environment of the battery pack hence influences its selectivity. In this study as shown in Table 2, seven PCMs with different thermophysical properties were integrated respectively with the LIB.

Table 2. Thermophysical properties of selected PCMs [45]

| PCM | RT24 | RT31 | RT35 | RT38 | RT42 | RT47 | RT50 | Unit |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Density | 770 | 760 | 770 | 750 | 760 | 770 | 880 | kg/m3 |
| Specific heat | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | J/kg∙K |
| Thermal conductivity | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | W/m∙K |
| Dynamic viscosity | 0.02 | 0.02 | 0.02 | 0.02 | 0.02 | 0.02 | 0.02 | kg/m∙s |
| Pure melting heat | 160000 | 165000 | 160000 | 170000 | 165000 | 160000 | 160000 | J/kg |
| Solidification temperature | 21 | 29 | 32 | 34 | 38 | 41 | 45 | ℃ |
| Melting temperature | 25 | 34 | 38 | 39 | 43 | 48 | 51 | ℃ |

Besides, the varied thermophysical properties of the PCMs, thermophysical properties of the shell material such as thermal conductivity and density influences the thermal control ability of the LIB/PCM system. In this study, four different shell materials, shown in Table 3, were selected for performance comparison.

Table 3. Thermophysical properties of selected shell materials.

| Material | Al | Steel | epoxy | Cu | Unit |
| --- | --- | --- | --- | --- | --- |
| Density | 2719 | 8030 | 1255 | 8978 | kg/m3 |
| Specific heat | 871 | 502.48 | 1745 | 381 | J/kg∙K |
| Thermal conductivity | 202.4 | 16.27 | 0.34 | 387.6 | W/m∙K |

To optimize the thermal management capability of LIB/PCM system, the effect of heat transfer coefficient between the shell and the ambient on system performance was evaluated at values of 1 W/m2K, 5 W/m2K and 10 W/m2K respectively. To evaluate the effect of PCM fill volume on system temperature during charging and discharging, LIB/PCM system with PCM volume ratio of 100%, 70%, 40%, 10% and 0% were used. As shown in Figure 3, the PCM volume ratio refers to the ratio between the actual volume of PCM filled and the maximum volume of PCM that can be filled in the LIB/PCM system.

Figure 3. LIB/PCM system showing PCM volume ratios of (a) 0%, (b) 70%, and (c) 100%.

3. The Numerical Model

The 3D convection and diffusion of the PCM phase change process required melting and solidification models based on finite volume method (FVM) [46]. The enthalpy porosity method was used in ANSYS Fluent to simulate the melting of the PCM. With this method, the liquid fraction was calculated within the computational domain instead of tracking the melt interface front end. The liquid fraction was the amount of cell volume in liquid form. The change of melt fraction with the melting process was between 0 and 1, which represented the solid PCM and the liquid PCM after the transformation. Based on this method, the following were assumed for the PCM [47]:

- The PCM was assumed to be homogeneous and isotropic.

- The thermophysical properties of PCM were uniform throughout its volume.

- The flow of the melted PCM fluid was laminar and the fluid assumed to be an incompressible Newtonian fluid.

- The PCM was assumed to be an inviscid fluid after melting.

- The radiation in the heat transfer process was ignored.

- The thermophysical properties of PCM were assumed to be constant, but the density was approximated using the Boussinesq approximation, where the ratio of ∆ρρ  is less than 1. The Boussinesq approximation considered buoyancy in the natural convection processes.

3.1. Governing equations

Continuity, energy, and momentum were mainly considered in the simulation of the LIB/PCM system during the charging and discharging process. When conducting CFD simulation, boussinesq approximation provides the foundation for the simulation [48]. The continuity and momentum equations are given by equations (1-4) [47]:

∂u∂t+∂ρu∂x+∂ρv∂y+∂ρw∂z=0#1

∂ρu∂t+∂ρuu∂x+∂ρvu∂y+∂ρwu∂z=-∂P∂x+∂∂xμ∂u∂x+∂∂yμ∂u∂y+∂∂zμ∂u∂z+Sx#2

∂ρv∂t+∂ρuv∂x+∂ρvv∂y+∂ρwv∂z=-∂P∂y+∂∂xμ∂v∂x+∂∂yμ∂v∂y+

∂∂zμ∂v∂z+Sy+ρgβT-Tm#3

∂ρw∂t+∂ρuw∂x+∂ρvw∂y+∂ρww∂z=-∂P∂x+∂∂xμ∂w∂x+∂∂yμ∂w∂y

+∂∂zμ∂w∂z+Sz#4

where Sx, Sy and Sz are the momentum source terms in x,  y and z direction respectively, suitable for the phase change process when convection is considered. Sx=Amushy(1-λ)2λ3+εu, Sy=Amushy(1-λ)2λ3+εv, Sz=Amushy(1-λ)2λ3+εw, u is the velocity in x-direction, v is the velocity in y-direction, w is the velocity in z-direction, t is time, ρ is density, P is performance score, μ is dynamic viscosity, g is gravitational acceleration, β is thermal expansion coefficient, T is temperature. Amushy is mushy zone constant, which can be changed from 104 to 107, and in ANSYS Fluent, an enthalpy porosity technique is used. Here, 105 was chosen as the mushy zone constant, λ is the liquid volume fraction, ε is a constant which was used to prevent the equation from being divisible by 0, and in this study，ε was set to 0.001[48].

The energy equation is given by Equation (5):

∂ρH∂t+∂ρuH∂x+∂ρvH∂y+∂ρwH∂z=∂∂xk∂T∂x+∂∂yk∂T∂y+∂∂zk∂T∂z#5

where the specific enthalpy H=h+∆H, h=href+TrefTCpdT+λL, h is sensible enthalpy, k is thermal conductivity, ∆H is latent heat content of PCM, href is reference enthalpy, Tref is reference temperature of PCM,  Cp is specific heat, L is latent heat. Since during the charging and discharging of the PCM, an operating temperature change can lead to severe phase transformation, the liquid fraction, λ was made to change with temperature as follows:

λ=0 if TPCM<Tsolidus, λ=1 if TPCM>Tliquidus, and λ=TPCM-TsolidusTliquidus-Tsolidus if Tsolidus<TPCM<Tliquidus.

3.2.  Initial and boundary conditions

The initial condition was Tx, y,z=T0 when t=0. The boundary condition at the interface between the battery and PCM was calculated using equation (6) [47]:

-kb∂Tb∂η=-kPCM∂TPCM∂η#6

The boundary condition at the interface between the PCM and container was calculated using equation (7) [48]:

-kPCM∂TPCM∂η=-kc∂Tc∂η#7

The boundary condition between the container and the ambient (natural convection) was determined by equation (8) [47]:

-kc∂Tc∂η=hTc-T0#8

The boundary condition between the top of battery pack and the ambient (natural convection) was calculated using equation (9) [47]:

-kb∂Tb∂η=h0Tb-T0#9

The boundary condition between the PCM and the ambient (natural convection) was determined by equation (10) [48]:

-kPCM∂TPCM∂η=hTPCM-T0#10

where kb, kPCM and kc are the thermal conductivity of the battery, PCM and container respectively;  Tb, TPCM and Tc are respectively the temperature of the battery, PCM and container. h is the convective heat transfer coefficient between the shell and the ambient, and between PCM and the ambient, which was set to 5 W/m2K unless otherwise specified. T0 is the ambient temperature and it was set to 20 ℃ throughout the simulation unless otherwise specified. h0 is the convective heat transfer coefficient between the top of battery pack and the ambient, and because it was assumed to be a heat insulation, h0 was set to 0 W/m2K.

3.3. Heat generation of LIB

For LIB, the energy conservation in three-dimension was determined by equation (11) [45]:

ρbCpb∂TL∂t=λrr∂∂rr∂TL∂r+λφr2∂2TL∂φ2+λZ∂2TL∂Z2+Q                             (11)

Where ρb is the density of LIB, Cpb is the specific heat capacity of the battery, TL is the local temperature, t means time, λr, λφ and λZ are the thermal conductivity coefficients in three direction in a cylindrical coordinate system, Q is the heat generation rate of LIB.

The heat generation rate was calculated using equation (12) from Bernardi et al. [38]:

Q=IUOCV-U+TL∂UOCV∂TL                                                        (12)

Where I is charge and discharge current, UOCV is open circuit voltage and U is cell potential, I(UOCV-U) is the heat generation due to the Joule resistance of the battery, ∂UOCV∂TL is the entropy coefficient caused by the electrochemical reactions in the cell and is equal to 0.4 mv/k [49].

Because the heat generation was assumed to be uniform, the heat generation per volume of LIB was calculated using equation (13) [50]:

q=1VUOCV-U+TL∂UOCV∂TL=1VIRj+TL∂UOCV∂TL                             (13)

Where q is volumetric heat generation rate, V is the volume of 18650 LIB, Rj is Joule resistance of the cell. When the charge and discharge rate was 2C, the value of q was determined to be 41788.37 W/m3.

4. Simulation setups

ANSYS 2022 R2 was used to simulate the thermal behaviour of the LIB/PCM system. 3D models of the battery pack, made using SolidWorks 2019 were imported and meshed in ANSYS 2022 R2 Workbench. Transient simulation was used to visualize the temperature change process with time during charging and discharging. Energy was considered in the model for the heat transfer along with a viscous model set to laminar. The solidification and melting functions were also turned on for the PCM phase transformation process. In the solution methods section for transient simulations, PISO scheme was selected. For an FVM method, the choice of grid was the staggered grid. Here for momentum and energy, second order upwind scheme and PRESTO! scheme was used to solve the pressure equation. In the solution control part, under-relaxation factors, 0.3, 1, 1, 0.7, 0.9,1 were set respectively for the pressure, density, body force, momentum, liquid fraction, and energy. For residuals, the criterion for energy was set to 10-6, and all other criteria set to 10-4. The maximum number of iterations performed in each time step was set to 20.

4.1. Grid and Time step size validation

To ensure the accuracy and reliability of the simulation results, grid size validation and time step size validation were carried out. For the LIB/PCM model, three different grid sizes shown in Table 4 were evaluated. The results of grid/mesh size validation and time step validation are shown in Figure 4. It can be seen from Figure 4(a) that the profile of Grid 2 with size 1.9 mm is in the middle of that of Grid 1 and Grid 3 both following a similar profile. For reasons of computational cost and accuracy, Grid 2 was selected for the simulation. Figure 5 shows the grid domain of the LIB/PCM model using Grid 2. To get the optimal time step, three different timestep ranging between 0.6 s to 1.8 s were evaluated. Based on the result shown in Figure 4(b), a time step of 1.2 s was chosen for the simulation to reduce computational costs without losing simulation accuracy.

Table 4. Grid size and number.

|  | Grid 1 | Grid 2 | Grid 3 |
| --- | --- | --- | --- |
| Grid size | 1.4mm | 1.9 mm | 2.4mm |
| Number of grids | 376151 | 150767 | 85266 |

Figure 4. (a) Grid size validation, and (b) timestep validation.

Figure 5. The figure of grid domain.

4.2. Model validation

Before using ANSYS2022 R2 to simulate the numerical model of the LIB/PCM unit, it was necessary to verify the effectiveness of the ANSYS simulation process. To verify the process, the simulation conducted by J. R. Patel and M. K. Rathod [33] was reproduced and compared to their results as shown in Figure 6. The figure shows the comparative result of the maximum static temperature in the LIB/PCM system model between J. R. Patel and M. K. Rathod's data and the present simulation results. It can be observed that high consistency exists between both results as depicted by the temperature profiles in Figure 6. The maximum difference observed between the two sets of temperature results was less than 1.5%, implying that the ANSYS simulation process is valid, hence the model can be used to study the LIB/PCM system.

Figure 6. Model validation.

5. Result and discussion

In Ansys 2022 R2, the charge and discharge process of the LIB/PCM system was simulated under six different variable conditions, i.e., the type of PCM wrapped in LIB, the working ambient temperature (Ta), the shell material, the heat transfer coefficient (h) between the ambient and the system, the volume of PCM and the arrangement of LIB/PCM system. In all simulations, the maximum temperature (Tmax) and temperature difference (∆T), the difference between the maximum and minimum temperature in the LIB/PCM system at a given moment, were recorded.

5.1. Effect of PCM under different ambient temperatures

The LIBs were fully wrapped respectively with the seven selected PCMs (RT24, RT31, RT35, RT38, RT42, RT47, RT50 - thermophysical properties shown in Table 2). They were then respectively simulated to undergo cyclic charging and discharging at three different ambient temperatures (Ta  equals to 20 ℃, 30 ℃ or 40 ℃) respectively under 2 C charge-discharge rate and constant heat transfer coefficient of 5 W/m2K as shown in Figure 7(a1, b1, c1). Also shown in Figure 7(a2, b2, c2) is the liquid fraction of the PCMs in charging-discharging mode at those three ambient temperatures.

Figure 7. Variation of LIB/PCM maximum temperature with the selected PCMs (a1), (b1), (c1) and the change of PCM liquid fraction (a2), (b2), (c2).

From Figure 7(a1, b1, c1), the Tmax increases with time during charging and discharging process at those conditions. The LIB pack containing PCM-RT24 achieved the maximum value of  Tmax at the end of the simulation time (t=150 min) while the LIB wrapped with PCM-RT50 achieved the lowest value. When the ambient temperature was 20 ℃, 30 ℃ and 40 ℃, the Tmax of the LIB pack with PCM-RT24 was respectively, 18.0%, 14.7% and 10.0% higher than that of the LIB pack with PCM-RT50 at t=150 min. The Tmax curves of the PCMs can be divided into two types. One type is with PCMs having phase transition temperatures lower than the ambient temperature (See Figure 7 and Table 2 for selected PCM melting points and the ambient temperatures), one example is shown with PCM-RT24, a PCM with a phase transition temperature lower than the ambient temperature Ta=30 ℃, as shown in Figure 7(b1). The Tmax curve for this PCM type shows a concave down profile with a positive gradient indicating an increasing temperature with time. It can be seen from the corresponding liquid fraction plot in Figure 7(b2) that the PCM-RT24 was in the liquid state during the whole process, indicating that it did not absorb latent heat through the charging and discharging process hence had very little inhibition on the temperature rise of the system. The other type was with PCMs having phase transition temperatures higher than the simulated ambient temperatures. The Tmax curves for PCMs under this condition shows an initial sharp rise in temperature before a transition stage where a gradual increase was observed over time. Figures 7(a2, b2, c2) show the liquid fraction of these PCMs during this phase transition period from solid to liquid before they turn to 100% liquid. Corresponding plots in Figures 7(a1, b1, c1) show that during the phase transition period, as the PCMs receive heat from the LIB, the temperature rises slightly. The moment all the solid PCM changes to liquid, plots in Figures 7(a1, b1, c1) show significant temperature rise till the Tmax reaches it maximum value. In Figure 7, it was also observed that PCMs with melting points above the ambient temperature and having higher phase transition temperatures had comparatively lower maximum value of  Tmax. So, the higher the PCM phase transition temperature the more effective control of the temperature rise.  Besides, it was also found from the liquid fraction plots that the higher the PCM phase transition temperature, the longer the phase transition time. The PCM observed with the longest phase transition time was 70 min, 60 min and 40 min longer than the PCM with the shortest phase transition time when the ambient temperatures were 20℃, 30℃ and 40℃ respectively. This is because the PCM with longer phase transition time absorbed more heat during the phase transition process hence had the capacity to control the temperature of the LIB/PCM system more effectively. In addition to the Tmax of the system, the temperature difference (∆T) between the maximum and minimum temperature in the LIB/PCM system affected system performance. Figure 8 shows the ∆T of the LIB/PCM system under the three ambient temperature conditions at t=150 min.

Figure 8. Temperature difference (∆T) of variable PCM under the three ambient temperature conditions.

Figure 8 demonstrates that in general, the LIBs wrapped with PCM with higher phase change temperature had smaller ∆T in the system after a period of charging and discharging. This is because the PCM with a higher phase change temperature can absorb more heat to control the temperature rise of the LIB/PCM system hence reducing the ∆T. It is important that the chosen PCM for wrapping LIB has its phase temperature coinciding with the optimal operating temperature range (20℃ to 40℃) of the LIB. It can be seen in Figure 8 that the ∆T of the system using the same PCM generally increases with increasing ambient temperature. It can be concluded that the LIB system using PCM for cooling purposes may not be suitable under high ambient temperatures.

When the ambient temperature was 20 °C, the temperature of PCM-RT35 maintained the longest time in the range of 20 to 40 ℃, reaching 67 minutes, much longer than 22 minutes spent by PCM-RT50 with the highest phase temperature. This means that under this ambient temperature, PCM-RT35 absorbed more heat during the phase transition enabling it to better control the temperature of the LIB/PCM system. When the ambient temperature was 30 °C, the phase transition temperature of PCM-RT35 was in the range of 30-40 ℃ and reached 50 minutes in this temperature region, about 6 times longer than that of PCM-RT50. Therefore, irrespective of the ambient temperature being 20 or 30℃, PCM-RT35 appears to be a suitable choice for the LIB/PCM system. When the ambient temperature was set to 40°C, PCM-RT47 maintained a phase transition temperature below 50°C albeit for a comparatively shorter time. In contrast, PCM-RT50 showed a longer phase change time and capacity to control the temperature longer. However, the phase change temperature of PCM-RT50 was observed to be high, which further reduces the performance of the system. To better evaluate the effect of these two PCMs on the performance of the LIB, a Weighted Product Method (WPM) [27] was used (See Table 5). With this method, several attributes of different weights are specified. Each attribute represents the corresponding variable, and the sum of the weights of these attributes are equal to one (or 100%). The comprehensive performance score of the alternative is then determined by equation (11):

Pi=j=1M[mijnormal]wj                                                        (11)

Where Pi is the overall or composite score of the alternative Ai, (mij)normal is the normalized value of mij, and the choice with the highest Pi value is considered as the best choice.

These attributes can be positive or negative. Once the contribution value of the attribute is confirmed to be available, the normalized values can then be calculated by mijK/(mij)L, where (mij)K is the attribute metric of the K-th alternative, and (mij)L is the attribute metric of the L-th alternative, which has a higher attribute metric among the considered alternatives. This ratio is only valid for beneficial attributes such as lower temperature difference (ΔT) in this study. And non beneficial attributes are a lower metric that is desirable, and the normalized value calculated by mijL/(mij)K.

When choosing ambient temperature as the variable parameter, the Tmax of the LIB/PCM system was considered a decisive factor that affects the life of the LIB [51]. In this case, it was assumed that the proportions of Tmax and ∆T were 70% and 30%, respectively.

Table 5. WPM applied to PCM RT47 and RT50 at Ta=40 ℃.

| PCM | Tmax (℃) | ∆T (℃) | M | N | P | Order |
| --- | --- | --- | --- | --- | --- | --- |
| RT47 | 95.83 | 10.2 | 0.96 | 0.95 | 0.96 | 2 |
| RT50 | 91.96 | 9.7 | 1 | 1 | 1 | 1 |

The WPM method constant M, N and P can be given by Equations (12-14):

M=TmaxminTmax#12

N=dTmaxmindTmax#13

P=M0.7N0.3#14

Therefore, based on the order shown in Table 4, PCM-RT50 can be regarded as the most suitable PCM when the ambient temperature is 40℃.

5.2 Effect of different shell materials

Table 3 shows the four selected shell materials and their varying thermophysical properties. This implies that the selected shell material for the LIB/PCM system can influence the performance of the entire system. In this section and as shown in Figure 9, the effect of different shell material on the thermal performance of the LIB/PCM system was carried out. Here the investigation was conducted at ambient temperature of 20 °C, under 2 C charge-discharge rate, constant heat transfer coefficient of 5 W/m2K and 100% PCM volume ratio. In Figure 9(a), the shell material’s thermal performance is shown while Figure 9(b) shows the corresponding liquid volume fraction of the PCM-RT42 used during the process. It is important to note that from Table 2, PCM-RT42 has melting point of 43 °C, 23 °C higher than the ambient temperature for this simulation.

Figure 9. (a) Variation of maximum temperature (Tmax) in the LIB pack with different shell materials, (b) Corresponding change of liquid volume fraction of PCM-RT42.

From the results in Figure 9(a), it can be observed that the Tmax profiles are similar. Between 0 to 20 minutes, because the Tmax in the LIB/PCM system was still lower than the melting point of the PCM-RT42, the PCM could not undergo the phase change process to absorb heat, so the Tmax rose sharply to nearly 40 °C. The liquid volume fraction curve in Figure 9(b) shows the PCM was in the fully solid state and did not absorb latent heat in the first 20 minutes. This shows as a corresponding temperature change up to about 40°C in Figure 9(a). After the first 20 minutes, the liquid volume fraction increased with time, and this reflected in Tmax increase for the various shell materials. Out of the four shell materials, Epoxy exhibited the highest Tmax of 77.2°C at t=150 min. In contrast, the system with Cu shell exhibited better temperature control by achieving the lowest Tmax of 70.55°C by t=150 min, 9.4% lower than the Epoxy. The maximum value of Tmax of the system with Al and Fe as shell materials was between that of Cu and Epoxy.  It can be seen in Figure 9(a) that at temperatures below 60 °C, the performance of LIB/PCM system under different shell materials is similar, and the Tmax shows obvious differences after 60 minutes. Figure 10 shows the temperature difference of LIB systems using different shell materials at t=150 min. From Figure 10, the LIB/PCM system using Cu as the shell material had the smallest ∆T of 9.1°C after multiple charge-discharge cycles. The ∆T with Al shell material was relatively closer to that of Cu, at 9.6°C. The Epoxy shell overall shows the largest ∆T value, more than two times that of the Cu shell. To select the optimal shell material for the LIB/PCM system, WPM was applied as shown in Table 6.

Figure 10. Temperature difference (∆T) of LIB/PCM system with different shell material.

Table 6. Order of shell material using WPM.

| Material | Tmax (°C) | ∆T (°C) | M | N | P | Order |
| --- | --- | --- | --- | --- | --- | --- |
| Al | 71.64 | 9.6 | 0.985 | 0.948 | 0.974 | 2 |
| Cu | 70.55 | 9.1 | 1 | 1 | 1 | 1 |
| Fe | 72.22 | 14.9 | 0.977 | 0.611 | 0.849 | 3 |
| Epoxy | 77.19 | 27.2 | 0.914 | 0.335 | 0.676 | 4 |

Based on the WPM result shown in Table 6, Cu with the lowest Tmax and smallest ∆T becomes the most suitable shell material for the LIB/PCM system. However, the performance of WPM using Al as the shell material was very close to that of Cu, and based on the CES software database, the cost and density of Al are about a quarter of that of Cu, so Al was selected as the shell material for this study. In practical applications, in addition to the Tmax and internal ∆T in the LIB/PCM system due to different shell materials, factors such as density, processability, and cost of the shell material etc may also be considered.

5.3 Effect of heat transfer coefficient

In this section, the influence of heat transfer coefficient (h) on the performance of LIB/PCM system was studied using PCM-RT42 with 100% volume ratio. Figure 11 shows the variation of the Tmax and liquid fraction in the system with heat transfer coefficient values of 1 W/m2K, 5 W/m2K and 10 W/m2K respectively.

Figure 11. Variation of heat transfer coefficient (h) with (a) maximum temperature (Tmax) and (b) liquid fraction at ambient temperature of 20°C.

Figure 11(a) shows that the variation of the heat transfer coefficient directly influences the Tmax of the LIB/PCM system. Here, there is an inverse relationship showing a larger heat transfer coefficient corresponding to a lower Tmax profile. The Tmax of the system shows an initial rapid increase to 40°C in 20 minutes for all heat transfer coefficient values simulated. The corresponding liquid fraction plot in Figure 11(b) shows that in the first 20 minutes, the PCM-RT42 absorbed heat in the solid state. After the first 20 minutes, it entered the transition state from solid to liquid and it was during this transition state that the influence of the heat transfer coefficient on the process became apparent. With a heat transfer coefficient of 1 W/m2K, Figure 11(a) shows a very sharp rise in the temperature of the LIB/PCM system. This sharp rise in temperature increased the rate at which the PCM-RT42 melted and hence as shown in Figure 11(b), the PCM reached the complete liquid state comparatively earlier than that with the other two heat transfer coefficients. After PCM-RT42 became liquid and completed the phase transition, it no longer absorbed latent heat, so the Tmax rose rapidly to 112.38°C at t=150 min. At this point, there was the likelihood of thermal runaway which can increase accident risk with the LIB/PCM system. With the heat transfer coefficient equal to 5 W/m2K, the comparative change in the temperature profile was milder than that with 1 W/m2K. Here, a longer phase transition time up to 80 mins was experienced, and the system Tmax reached 80.71°C, about 44.86% lower than that obtained with 1 W/m2K. This is because as the heat transfer coefficient increased, the ambient air absorbed more heat through thermal convection with the surface of the LIB/PCM system, thus effectively helping the PCM to control the temperature. When the heat transfer coefficient was set to 10 W/m2K, the temperature of the LIB/PCM system was relatively stable around the transition temperature. This resulted in the PCM-RT42 set to 10 W/m2K having the longest phase transition time, nearly four times that of the phase transition time with 1 W/m2K. Here, the maximum value of the Tmax in the system was 55.18°C, about 62.30% lower than the value obtained with 1 W/m2K. In addition to the Tmax, the ∆T was also analysed under different heat transfer coefficient as shown in Figure 12.  It shows that at 1 W/m2K, the system ∆T was 6°C, about 45.45% lower than the other two cases. When the heat transfer coefficient was set to 1 W/m2K, the maximum value of  Tmax was at its highest and its ∆T at its lowest in the proposed system, as demonstrated with the temperature contours of the LIB/PCM system in Figure 13.

Figure 12. Effect of heat transfer coefficient on temperature difference (∆T) of LIB/PCM system.

Figure 13. Temperature contour of the LIB/PCM system with different PCM volume.

To further evaluate the three cases, WPM was applied as shown in Table 7. According to the result shown in Table 7, when the heat transfer coefficient was 10 W/m2K, the LIB/PCM system showed the best thermal regulation capability. This is mainly because the greater the heat transfer coefficient, the more heat it is removed by natural convection leading to a stronger thermal management capability of the LIB/PCM system.

Table 7. Order of simulation group with different heat transfer coefficient.

| h (w/m2K) | Tmax (°C) | ∆T (°C) | M | N | P | Order |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 146.38 | 6 | 0.38 | 1 | 0.51 | 3 |
| 5 | 80.71 | 11 | 0.68 | 0.55 | 0.64 | 2 |
| 10 | 55.18 | 11 | 1 | 0.55 | 0.84 | 1 |

5.4 Effect of PCM volume ratio

The effect of fill volume ratio of the PCM on the thermal management capability of the system was studied by changing the volume ratio of PCM-RT42 in the LIB/PCM system. Figure 14 shows the variation of Tmax and liquid fraction respectively with different volume ratios (100%, 70%, 40%%, 10% and 0%) of PCM-RT42.

Figure 14. (a) Maximum temperature Tmax for different volume ratios of the LIB/PCM-RT42 system (b) the liquid fraction for different volume ratios of PCM-RT42.

Figure 14(a) shows the variation of PCM volume ratio in the LIB/PCM-RT42 system and its influence on Tmax. Since the PCM was the same but volume was varied, the Tmax profiles were similar for different PCM volume ratios. There was a sharp increase in the first 20 minutes due to the PCM being in its solid state. As the Tmax exceeded the melting point of PCM-RT42, a change from solid to liquid was observed as shown in Figure 14(b). Due to the varied volumes, the PCMs reached 100% liquid state at different times. During the transition process, PCM-RT42 accumulated a large amount of latent heat, thereby inhibiting the temperature rise of the LIB/PCM system. After the phase transition was completed, the temperature rose rapidly again as the PCM was unable to absorb latent heat hence lost its ability to suppress temperature. Figure 14(a) also shows that, in the first 80 minutes of simulation, the system with 100% PCM volume ratio had the lowest system temperature due to its large PCM volume and capacity to absorb more heat. In the first 60 minutes, it was observed that the larger the PCM volume ratio, the smaller the Tmax of the LIB/PCM system. However, this changed after about 110 minutes, evidenced by the system with 0% PCM volume ratio showing the lowest temperature. At the end of the simulation, the system with 100% PCM volume ratio had the highest Tmax. As the volume ratio of PCM in the LIB/PCM system decreased, the temperature at the end of the simulation also gradually decreased. From Figure 14(b), the higher volume ratio of PCM, the longer the phase transition time. For the system with 0% PCM volume ratio, the temperature in the first 60 minutes was the highest as it could not absorb the heat. However, after 60 minutes, the temperature remained stable and finally this PCM achieved the lowest Tmax at the end of the simulation. Based on the changes in the Tmax and liquid fraction curves of these LIB/PCM systems, it can be summarized that, the larger the PCM volume ratio, the more latent heat it absorbs during PCM phase transition, resulting in a lower Tmax. When the PCM phase changed completely, Tmax continued to rise with the PCM in the liquid state, hence systems with higher PCM volume ratios had inhibitory effect on the heat dissipation of the LIB. Therefore, to better manage the thermal performance of LIB and maintain the system temperature at a relatively low temperature during use, the battery pack with different PCM volume ratios can be selected based on the required charging and discharging time of the LIB. For example, if it is necessary to ensure that the maximum temperature of the system remains below 45 °C after 80 minutes of charging and discharging, a battery pack with 100% PCM content needs to be selected. If it is necessary to ensure that the maximum temperature of the system remains below 55 °C after 150 minutes of charging and discharging, a battery pack without PCM can be selected.

Correspondingly, Figure 15 shows the temperature contours of LIB/PCM system. Here, the temperature distribution for different PCM volume ratio was relatively uniform at different times. The temperature difference between PCM and LIB did not change significantly with increase in charging and discharging time.

Figure 15. Temperature contour of the LIB/PCM system with different PCM volume.

The ∆T of the LIB/PCM system with different PCM volume ratio is shown in Figure 16. It can be observed that the higher the PCM volume ratio, the larger the ∆T  in the LIB/PCM system, demonstrating that the addition of the PCM can be harmful to its thermal management. In practical applications, different PCM volume ratios can be selected according to different requirements of the system.

Figure 16. Temperature difference (∆T) of the LIB/PCM system with different PCM volume ratio.

5.5 Effect of battery arrangement shape on battery thermal management system (BTMS)

The shape and configuration of the battery leads to different heat transfer area between the system and the environment even though the three shapes of the model have almost the same volume. To evaluate the influence of LIB/PCM configuration on thermal performance, PCM-RT42 with 100% volume ratio in the LIB/PCM system was used. The reference conditions for the simulation was 20 °C ambient temperature, 2 C charge-discharge rate and constant heat transfer coefficient of 5 W/m2K. Figure 17 shows the Tmax in the LIB/PCM system and liquid fraction of the LIB/PCM system with square, circular, and rectangular configurations and corresponding lateral areas of 22620 mm2, 20012 mm2 and 23140 mm2 respectively.

Figure 17. Performance variation of LIB configurations (a) Maximum temperature difference (Tmax) (b) liquid fraction of PCM-RT42 in the LIB/PCM system

From Figure 17(a), the rectangular LIB/PCM system configuration maintained a comparatively lower Tmax profile during the transition stage. In the first 20 minutes, the rectangular LIB/PCM system was in the solid state and absorbed heat from the LIB. The next 50 minutes, as observed in Figure 17(b), shows the PCM-RT42 went through phase transition till it reached 100% liquid fraction. In the 100% liquid state, no heat was absorbed, and the temperature rose rapidly to 71.64 °C. The circularly configured LIB/PCM system as shown in Figure 17(a) attained the fastest rise to the highest Tmax value amongst all three configurations. Figure 17(b) shows that it completed the phase transition 5 minutes earlier than that of the rectangular LIB/PCM system configuration. The comparatively sharp rise in Tmax for this circularly configured LIB/PCM system led to a Tmax of 14.78 °C higher than that of rectangular LIB/PCM system, and a 1.08 °C higher than that of the squarely configured LIB/PCM system. Measurement of the lateral areas of LIB systems for these three shapes in SolidWorks shows the lateral area of the rectangular LIB/PCM system is 520 mm2 more than that of the square shaped system and 3128 mm2 more than the circular system. Combining the analysis of the temperature data of the three systems, it can be inferred that the larger the lateral area, the better the heat dissipation.

Figure 18 shows the ∆T of the LIB/PCM pack in the three configurations at t=150 min. Here, the rectangular LIB/PCM system had the smallest ∆T of 9.6 °C, comparatively lower than that of the circular and square shaped systems. Therefore, it can be concluded that the configuration of an LIB/PCM system with larger side area can reduce the ∆T in the system by promoting the heat dissipation of the system. Based on above analysis, the LIB/PCM system with rectangular shape was found to be the optimal choice for the thermal management of the LIB.

Figure 18. Temperature difference (∆T) of the LIB system in rectangular, square, and circular configurations.

6. Conclusion

To avoid thermal runaway and to ensure the correct operation of lithium-ion battery system, seven different of phase change materials having different thermophysical properties were integrated with varied configurations of lithium-ion battery/phase change material system to investigate their battery thermal management potential. Using ANSYS 2022R2 the impacts of shell material, heat transfer coefficient, phase change material volume ratio and the shape of the battery pack on the thermal performance of the lithium-ion battery/phase change material system were theoretically evaluated. The theoretical results show that:

- The lithium-ion battery/phase change material battery packs were found not to be suitable at high working temperatures. Phase change material-RT35 had the most potential for controlling the temperature in a suitable range for lithium-ion battery operation when the ambient temperature was 20 or 30 °C. Phase change material-RT50 was found to be more suitable for temperature control when the ambient temperature was 40°C.

- The lithium-ion battery /phase change material system with Cu shell material had the best temperature control effect on the system because the shell made using Cu provides the lowest temperature and smallest ∆T for the battery pack. However, because Al has great advantages over Cu in terms of cost, quality, and oxidation resistance, and the performance gap between Al and Cu in the simulation was not very significant, Al may be the best choice for practical applications.

- The larger the heat transfer coefficient, the more stable the lithium-ion battery/phase change material system can maintain a relatively lower operating temperature. The phase transition time of LIB/PCM system with a heat transfer coefficient of 10 W/m2K was almost four times that of 1 W/m2K. Here, the maximum temperature was found to be 55.18 °C, approximately 62.30% lower than the value obtained with a heat transfer coefficient of 1 W/m2K after 150 minutes of charging and discharging.

- The larger phase change material volume ratio in a lithium-ion battery /phase change material system, the larger ∆T in the system. This large volume ratio after the phase transition potentially hinders the heat dissipation of the proposed system.

- With almost the same volume, the rectangular lithium-ion battery/phase change material system had the lowest maximum temperature and the smallest temperature difference compared with the circular and square lithium-ion battery/phase change material system. The maximum temperature of the rectangular LIB/PCM system after 150 minutes of charging and discharging was 14.78 °C higher than that of the circular LIB/PCM. The minimum temperature difference obtained here was about 9.6 °C.

| Nomenclature |  |  |  |
| --- | --- | --- | --- |
| Amush | mush zone constant (kg/m3∙S) | v | y-velocity (m/s) |
| Cp | specific heat (J/Kg∙K) | w | z-velocity (m/s) |
| H | latent enthalpy (J/kg) | Greek symbols |  |
| ∆H | latent heat content (J/kg) | ρ | density (kg/m3) |
| h | sensible enthalpy (J/kg) | μ | dynamic viscosity (kg/m∙s) |
| k | thermal conductivity (W/m∙K) | β | thermal expansion coefficient (℃-1) |
| L | latent heat (J/kg) | λ | liquid fraction |
| g | gravitational acceleration (m/s2) | Subscripts |  |
| P | performance score | max | maximum |
| S | momentum source term | x | x-direction |
| T | temperature (℃) | y | y-direction |
| ∆T | temperature difference in LIB/PCM system (℃) | z | z-direction |
| t | time (s) |  |  |
| u | x-velocity (m/s) |  |  |

Conflicts of interest

The authors declare no conflict of interest.

Acknowledgment

This work was financially supported by Ningbo Science and Technology Innovation 2025 Megaproject under project code 2022Z154, and the Zhejiang Provincial Key Laboratory for Carbonaceous Wastes Processing and Process Intensification Research funded by the Zhejiang Provincial Department of Science and Technology (2020E10018). The authors also acknowledge the financial support from Nottingham Ningbo China Beacons of Excellence Research and Innovation Institute.

Reference

[1] M. Ahmad, Z.-Y. Zhao, Empirics on linkages among industrialization, urbanization, energy consumption, CO2 emissions and economic growth: a heterogeneous panel study of China, Environmental science and pollution research international, 25(30) (2018) 30617-30632.

[2] T. Jia, Y. Dai, R. Wang, Refining energy sources in winemaking industry by using solar energy as alternatives for fossil fuels: A review and perspective, Renewable and Sustainable Energy Reviews, 88 (2018) 278-296.

[3] R. P. Langford, K. Gillingham, Quantifying the benefits of the introduction of the hybrid electric vehicle, International Journal of Industrial Organization, 87 (2023) 102904.

[4] X. Lü, S. Li, X. He, C. Xie, S. He, Y. Xu, J. Fang, M. Zhang, X. Yang, Hybrid electric vehicles: A review of energy management strategies based on model predictive control, Journal of Energy Storage, 56 (2022) 106112.

[5] J. Kim, J. Oh, H. Lee, Review on battery thermal management system for electric vehicles, Applied Thermal Engineering, 149 (2019) 192-212.

[6] N. Ghaeminezhad, Z. Wang, Q. Ouyang, A Review on lithium-ion battery thermal management system techniques: A control-oriented analysis, Applied Thermal Engineering, 219 (2023) 119497.

[7] P. H. Andersen, J. A. Mathews, M. Rask, Integrating private transport into renewable energy policy: The strategy of creating intelligent recharging grids for electric vehicles, Energy policy, 37(7) (2009) 2481-2486.

[8] Z. Wang, X. Li, G. Zhang, Y. Lv, C. Wang, F. He, C. Yang, C. Yang, Thermal management investigation for lithium-ion battery module with different phase change materials, RSC advances, 7(68) (2017) 4299-42918.

[9] G. Jie, Z. Liangheng, L. Yan, S. Fan, W. Bin, H. Cunfu, Ultrasonic guided wave measurement and modeling analysis of the state of charge for lithium-ion battery, Journal of Energy Storage, 72 (2023) 108384.

[10] C. Li, H. Zhang, P. Ding, S. Yang, Y. Bai, Deep feature extraction in lifetime prognostics of lithium-ion batteries: Advances, challenges and perspectives, Renewable and Sustainable Energy Reviews, 184 (2023) 113576.

[11] Y. Yang, R. Wang, Z. Shen, Q. Yu, R. Xiong, W. Shen, Towards a safer lithium-ion batteries: A critical review on cause, characteristics, warning and disposal strategy for thermal runaway, Advances in Applied Energy, 11 (2023) 100146.

[12] Z. Li, Y. Guo, P. Zhang, Effects of the battery enclosure on the thermal behaviors of lithium-ion battery module during thermal runaway propagation by external-heating, Journal of energy storage, 48 (2022) 104002.

[13] A. O. Christopher Lee, A. S. I. S. Said, Impact of state of charge and cell arrangement on thermal runaway propagation in lithium ion battery cell arrays, Transportation Research Record, 2673(8) (2019) 408-417.

[14] X. Liu, C.-F. Zhang, J.-G. Zhou, X. Xiong, Y.-P. Wang, Thermal performance of battery thermal management system using fins to enhance the combination of thermoelectric Cooler and phase change Material, Applied energy, 322 (2022) 119503.

[15] Z. Wang, T. He, H. Bian, F. Jiang, Y. Yang, Characteristics of and factors influencing thermal runaway propagation in lithium-ion battery packs, Journal of Energy Storage, 41 (2021) 102956.

[16] R. Zhao, J. Liu, J. Gu, Simulation and experimental study on lithium ion battery short circuit, Applied energy, 173 (2016) 29-39.

[17] A. W. Golubkov, S. Scheikl, R. Planteu, G. Voitic, H. Wiltsche, C. Stangl, G. Fauler, A. Thaler, V. Hacker, Thermal runaway of commercial 18650 Li-ion batteries with LFP and NCA cathodes - impact of state of charge and overcharge, RSC advances, 5(7) (2015) 57171-57186.

[18] Q. Wang, P. Ping, X. Zhao, G. Chu, J. Sun, C. Chen, Thermal runaway caused fire and explosion of lithium ion battery, Journal of power sources, 208 (2012) 210-224.

[19] A. A. Pesaran, Battery thermal models for hybrid vehicle simulations, Journal of power sources, 110(2) (2002) 377-382.

[20] Y. Ye, L. H. Saw, Y. Shi, A. A. O. Tay, Numerical analyses on optimizing a heat pipe thermal management system for lithium-ion batteries during fast charging, Applied thermal engineering, 86 (2015) 281-291.

[21] Z. Y. Jiang, Z. G. Qu, Lithium–ion battery thermal management using heat pipe and phase change material during discharge–charge cycle: A comprehensive numerical study, Applied energy, 242 (2019) 378-392.

[22] M. Shahjalal, P. K. Roy, T. Shams, A. Fly, J. I. Chowdhury, M. R. Ahmed, K. Liu, A review on second-life of Li-ion batteries: prospects, challenges, and issues, Energy, 241 (2022) 122881.

[23] Z. Ling, F. Wang, X. Fang, X. Gao, Z. Zhang, A hybrid thermal management system for lithium ion batteries combining phase change materials with forced-air cooling, Applied energy, 148 (2015) 403-409.

[24] A. Babapoor, M. Azizi, G. Karimi, Thermal management of a Li-ion battery using carbon fiber-PCM composites, Applied Thermal Engineering, 82 (2015) 281-290.

[25] M. Chen, Y. Cui, D. Ouyang, J. Weng, J. Liu, L. Zhao, J. Wang, Experimental study on the hybrid carbon based phase change materials for thermal management performance of lithium‐ion battery module, International journal of energy research, 46(12) (2022) 17247-17261.

[26] S.-B. Zhang, X. He, N.-C. Long, Y.-J. Shen, Q. Gao, Improving the air-cooling performance for lithium-ion battery packs by changing the air flow pattern, Applied Thermal Engineering, 221 (2023) 119825.

[27] Z. Rao, S. Wang, G. Zhang, Simulation and experiment of thermal energy management with phase change material for ageing LiFePO4 power battery, Energy Conversion and Management, 52(12) (2011) 3408-3414.

[28] Y. Azizi, S. M. Sadrameli, Thermal management of a LiFePO4 battery pack at high temperature environment using a composite of phase change materials and aluminum wire mesh plates, Energy conversion and management, 128 (2016) 294-302.

[29] J. S. J. Zhao, B. Zhang, S. Wang and W. Wu, Automobile Applied Technology, 179 (2016) 601-608.

[30] A. Anisha, A. Kumar, Identification and Mitigation of Shortcomings in Direct and Indirect Liquid Cooling-Based Battery Thermal Management System, Energies (Basel), 16 (2023) 3857.

[31] P. Dubey, G. Pulugundla, A. K. Srouji, Direct Comparison of Immersion and Cold-Plate Based Cooling for Automotive Li-Ion Battery Modules, Energies, 14 (2021) 1259.

[32] G. Pulugundla, P. Dubey, A. Srouji, Time-Accurate CFD Analysis of Liquid Cold Plates for Efficient Thermal Performance of Electric Vehicle Li-Ion Battery Modules, SAE Technical Paper, 2019-01-0500, (2019).

[33] J. R. Patel, M. K. Rathod, Phase change material selection using simulation-oriented optimization to improve the thermal performance of lithium-ion battery, Journal of energy storage, 49 (2022) 103974.

[34] W. Wu, W. Wu, S. Wang, Thermal optimization of composite PCM based large-format lithium-ion battery modules under extreme operating conditions, Energy conversion and management, 153 (2017) 22-33.

[35] S. K. Kumar, A. a. B. M. Abduh, O. Sabih, R. Yazami, Temperature Effect on "Ragone Plots" of Lithium-Ion Batteries, Journal of the Electrochemical Society, 165(3) (2018) A674-A679.

[36] S. Sudhakaran, M. Terese, Y. Mohan, A. D. Thampi, S. Rani, Influence of various parameters on the cooling performance of battery thermal management systems based on phase change materials, Applied Thermal Engineering, 222 (2023) 119936.

[37] S. Mousavi, A. Zadehkabir, M. Siavashi, X. Yang, An improved hybrid thermal management system for prismatic Li-ion batteries integrated with mini-channel and phase change materials, Applied energy, 334 (2023) 120643.

[38] Q. Huang, X. Li, G. Zhang, Y. Kan, C. Li, J. Deng, C. Wang, Flexible composite phase change material with anti-leakage and anti-vibration properties for battery thermal management, Applied energy, 309 (2022) 118434.

[39] J. Weng, X. Yang, G. Zhang, D. Ouyang, M. Chen, J. Wang, Optimization of the detailed factors in a phase-change-material module for battery thermal management, International journal of heat and mass transfer, 138 (2019) 126-134.

[40] J. Luo, H. Gu, S. Wang, H. Wang, D. Zou, A coupled power battery cooling system based on phase change material and its influencing factors, Applied energy, 326 (2022) 119917.

[41] Z. Sun, R. Fan, F. Yan, T. Zhou, N. Zheng, Thermal management of the lithium-ion battery by the composite PCM-Fin structures, International journal of heat and mass transfer, 145 (2019) 118739.

[42] A. G. Mohammed, K. E. Elfeky, Q. Wang, Thermal management evaluation of Li-ion battery employing multiple phase change materials integrated thin heat sinks for hybrid electric vehicles, Journal of Power Sources, 516 (2021) 230680.

[43] S. He, B. Xiong, H. Lei, K. Dong, S. A. Khan, J. Zhao, Optimization of low-temperature preheating strategy for Li-ion batteries with supercooling phase change materials using response surface method, International Communications in Heat and Mass Transfer, 142 (2023) 106635.

[44] V. G. Choudhari, A. S. Dhoble, S. Panchal, Numerical analysis of different fin structures in phase change material module for battery thermal management system and its optimization, International journal of heat and mass transfer, 163 (2020) 120434.

[45] N. D. Rubitherm Gmbh, https://www.rubitherm.eu/en/index.php/productcategory/organische-pcm-rt.

[46] A. R. Bais, D. G. Subhedhar, N. C. Joshi, S. Panchal, Numerical investigation on thermal management system for lithium ion battery using phase change material, Materials Today: Proceedings, 66 (2022) 1726-1733.

[47] R. Moreira, J Palau, X. Sun, Simultaneous heat and mass transfer during the deep fat frying of tortilla chips, Journal of Food Process Engineering, 18 (1995) 307-320.

[48] R. D. Jilte, R. Kumar, M. H. Ahmadi, L. Chen, Battery thermal management system employing phase change material with cell-to-cell air cooling, Applied thermal engineering, 161 (2019) 114199.

[49] S. Al-Hallaj, J. R. Selman, Thermal modeling of secondary lithium batteries for electric vehicle/hybrid electric vehicle applications, Journal of power sources, 110 (2002) 341-348.

[50] D. Bernardi, E. Pawlikowski, J. Newman, GENERAL ENERGY BALANCE FOR BATTERY SYSTEMS, Journal of the Electrochemical Society, 132 (1985) 5-12.

[51] U. Morali, A numerical and statistical implementation of a thermal model for a lithium-ion battery, Energy (Oxford), 240 (2022) 122486.