(

Dependence of Magnetisation near Saturation on Alloying Content in Ferromagnetic Steel

G. H. Shirkoohi, Member, IEEE

Abstract— This paper shows that there is strong dependence of saturation magnetisation to the alloying content in ferromagnetic steels. This dependence was used to determine the cross-sectional areas of the commercial non-oriented and grain-oriented silicon-iron steels. The relationship for magnetisation near saturation to that of the contents of silicon and aluminium for a large number of steel samples was experimentally obtained using an air-cored magnetising system. Influence of approach to magnetic saturation and its use in the determination of the cross-sectional area of electrical steel strips using saturation magnetisation method was estimated. Standard deviation of cross-sectional area obtained using saturation magnetisation method was of the order of 0.14%. Standard deviation for using conventional technique was also of the similar order of around 0.11%.

Index Terms— Saturation magnetisation Electrical steel Alloying content Steel thickness Gamma ray absorption gauging Magnetic weighting.

# INTRODUCTION

S

ilicon-iron steel is still one of the best materials for applications in electric motors generators transformers electromagnets relays and other electromagnetic devices. In all the applications low iron loss and its constituent components hysteresis and eddy current losses are of prime importance. Determination of power loss is normally made on the Epstein samples of silicon-iron steel [1] and single sheets. Accuracy of the results greatly relies on the accurate setting of magnetic flux in the samples. This in turn requires an accurate measurement of cross-sectional areas or thicknesses of the samples if their widths can be accurately obtained. Some of the methods used for the determination of cross-sectional areas or thicknesses of silicon-iron steel are briefly reviewed below. Using eddy current methodology the thickness of silicon-iron steel is measured by observing the changes in the magnetic field caused by the eddy currents in steel [2-4]. The density method has been widely used to measure the average cross-sectional area such as that of the Epstein samples of precise size (length and width) in laboratories. The reproducibility of cross-sectional areas obtained using density method is characterised by a standard deviation of the order of 0.2% to 0.3% [1]. Thickness of the steel was determined from measurement of the equivalent magnetic reluctance of the magnetic circuit by Potanin [5]. Using the detection of time intervals between ultrasonic pulses produced and reflected from the surfaces of silicon-iron steel in accordance with the Lorentz force in an electromagnetic field the thickness of the steel plates between 1 mm and 4 mm was accomplished by means of a measurement technique by filtering the received waveform within a frequency region [6-9]. With the increasing emphasis on improving product quality many factories measure the thickness of silicon-iron steels on a production line using either transmission or back scatter (reflection) type radiation methods [10-13]. Automatic non-contact measurements of the thicknesses of plastic and steel sheets were also reported using laser [14, 15]. Nevertheless the varieties of methods used for the determination of cross-sectional areas or thicknesses of silicon-iron steels are not always convenient for utilisation under plant operating conditions. Radiation method is awkward and requires specially trained operators. Eddy current method is sensitive to the conductivity of the samples. An increase of 1 per cent in conductivity which can be easily caused by temperature change local cold working or heating treatment variations can cause a 1 per cent deviation in thickness [16]. Although a non-contact method sensitivity of magnetic-ultrasonic method is low and it is not easy to use for the thin silicon-iron steel. Application techniques using lasers require clear smooth surface of the steel. With the exception of the density method that measures the cross-sectional area directly; all the other methods determine only the thickness of silicon-iron steel sheets. These methods also require measurement of the width in order to calculate the cross-sectional area. In this paper by studying the dependence of saturation magnetisation of silicon-iron steel on the depth of magnetic saturation, silicon and aluminium contents and grain orientation, a saturation magnetisation method was developed for the determination of the cross-sectional areas of the steel strips initially in the form of Epstein size samples. Although magnetic saturation has not been the subject of interest in the past, modern techniques in control and operation of rotating machines has lead to the development of new methods for their characterisation [17].

# Experimental set up

Apparatus was designed so that measurements could be made on Epstein-strip sized samples in order to enable a data base to be assembled so that magnetic saturation methods could be assessed in comparison with weighing and γ-ray absorption techniques [18, 19].

Figure 1. Experimental apparatus for measurement of saturation magnetisation of Epstein size steel samples. SW is a computer-controlled switch CT is a current transducer and NE is the main magnetising coil. NB and NH are B- and H- Coils and MB and MH are their respective air flux compensation windings.

Figure 1 shows the diagram of the apparatus and the measuring circuitry. The test frame consists of a magnetising coil a B coil and an H coil. Flux closure yokes were not used. The solenoid wound on a nonmagnetic former is 200 mm long, with the width and height of 54 mm and 31 mm, respectively. This magnetising coil of 3060 turns is capable of delivering some 100 kA/m at its centre. The excitation of an Epstein sample requires around 800 VA at a very low power factor of around 75 W. The B coil (of dimensions ≈ 30mm × 10mm × 10mm), positioned at the centre of the solenoid, is connected to an air flux compensating mutual inductor so that flux from the sample is detected but not air flux from the applied field i.e. M only. An H coil (constructed on a non magnetic former of dimensions ≈ 30mm× 25mm × 1mm) placed near the sample surface was also connected to a mutual inductor so that when the flux to this H coil was balanced out (with sample absent) the demagnetising field (sample present) could then be detected by this free from that of the applied field. Field measurements along the length of the solenoid showed good linearity of the field of at least 50 mm either side if the centre of B and H coils. The demagnetising field at applied field H of 100 kA/m was around 0.8 kA/m.

This arrangement enabled close track to be kept of the size of the demagnetising field arising as sample geometry was changed. This greatly facilitated the confident design of any engineered commercial system. Demagnetising factors can be either calculated or measured as may be convenient in each case. When using a fully compensated system the flux recorded is from sample polarisation alone and excludes the magnetising air flux and the effects of the demagnetising field. Excitation was at 50 Hz the supply waveform being uncritical. Figure 2 shows the experimental set-up for measurements and the observed waveforms, with quantities measured shown in Figure 2(b). MSaturation (Ms) was calculated from the formula V = 4 JSat n f A; where V = average voltage of compensated B coil n = number of turns of B coil f = supply frequency and A = cross section area of the B-coil. Magnetising current and the exact supply frequency were sensed during measurements. Although the apparatus was initially designed for on-line measurement of cross sectional area of laminated steels during manufacturing process it has also been used to determine the magnetic properties of these materials for a range of magnetisation intensities approaching those close to saturation in compliance with the law of approach.

# Saturation effects in electromagnetic devices

(a)                                                                                                      (b)

Figure 2. (a) Experimental set-up for measurement of saturation magnetisation of Epstein size steel samples; (b) The waveforms of external magnetic field induced voltage and internal magnetisation.

There has been a steady and growing interest in determination and prediction of the magnetic properties of electrical steels in the saturation region [20-23]. In the past it would have been of some interest to quantify these for practical reasons for example where high saturation effects occur in the tooth regions of rotating machines. The subjective exposure of these materials to high saturation due to inverter generated modulated variable frequency waveforms is also driving the need for the desire to determine their characteristics in much higher saturation regions than those charted in the past. There is also growing evidence that localised saturation in transformer may be responsible for much more undetected deterioration of performance and operation of energy and power network systems. Saturation effects within the nonlinear laminated cores is reported to be further enhanced by the intrinsic operational characteristics of power transformers resulting in the need for inclusion of additional more complex measures associated with saturation effects in modelling of these types of devices [24, 25]. The inter-laminar flow of flux well known to particularly occur in the overlap regions in corners and T-joint of laminated transformer cores is also seen to be radically affected by localised saturation in the core material [26]. Kefalas and Kladas reported regions of heavy saturation in transformer cores used in renewable energy systems which are not recognised by their manufacturers [27]. Study of iron core saturation in welding transformers resulting from unbalanced voltages generated by dc-dc converters has lead to design of appropriate preventive counter measures [28, 29]. Magnetic properties of laminated transformer cores were investigated under over-saturation conditions for determination of iron loss and excitation characteristics [30] and the development of modelling technique for saturation properties of laminated cores where a quasi-nonlinear approach is used to adequately solve industrial problems [31]. Jaiswal et al. used separate saturation magnetisation curves in order to predict losses in three-phase Induction Motors [32]. Similar studies were presented in the past for single-phase motors [33, 34] where localised flux conditions and losses were acceptably estimated using similar techniques. However although saturation in tooth tip and tooth root regions were considerable in the latter investigation the three-phase machines with grain-oriented cores investigated in the former study are expected to show far more localised saturation levels. Other work includes effect of severe uneven localised saturation magnetisation which is shown to occur in the core of widely used rectangular induction machines due to the core geometry instigated unbalanced phase currents [35]. Saturation magnetisation is also shown to be effective in non-destructive measurement of surface–hardening depth of steel where law of approach to saturation was used to determine the case depth of induction-hardened and carburised steel rods [36].

# Preparation of samples

## Determination of composition and cross section area

Table 1.

Conventional silicon and aluminium contents of the silicon-iron steel samples.

| Orientation | Nominal silicon content (%) | Nominal thickness (mm) | Si content (%) | S. D. (%) | Al content (%) | S. D. (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Non - oriented | 0.1 | variable 0.35 0.47 0.50 0.65 0.75 | 0.1080 | 6.9 | 0.0370 | 15 |
|  | 0.2 |  | 0.2202 | 7.6 | 0.0357 | 14 |
|  | 0.5 |  | 0.4744 | 7.8 | 0.1388 | 15 |
|  | 1.3 |  | 1.3133 | 1.3 | 0.1402 | 5 |
|  | 1.8 |  | 1.8074 | 1.5 | 0.3785 | 3 |
| Grain - oriented | 3 | 0.27 0.30 0.35 | 3.0086 | 1.8 | 0.0000 | 0 |

In accordance with British Standard [1] the Epstein samples used in the study were cut from various grades of commercially available non-oriented and grain-oriented silicon-iron steel produced by a factory at different period of time. The number of samples in an individual grade ranged from eleven to twenty one. All the samples were along the rolling direction and were also fully annealed.

Using chemical analysis method the contents of silicon and aluminium of the samples were analysed. As shown in Figure 3(a-f) the contents of both silicon and aluminium vary around the average or the so called conventional values of contents. Using statistical analysis the conventional contents of silicon and aluminium for each grade of samples are shown in table1. The standard deviation (S.D.) of silicon content in the grades is up to 7.8% while that of aluminium is seen to be up to 15%.

In accordance with British and IEC Standards [1] the cross-sectional areas, AS (=m/(l×d)) of these Epstein samples are determined using the density method. Densities of the samples are determined from their silicon and aluminium contents using:

(1)

where 7865 is the basic density value for electrical steel (kgm-3), and  are the weight percentages of silicon and aluminium contents of the samples.

Average thicknesses of the samples are then determined (=AS/width). Widths of the samples were precisely measured using a vernier micrometer of 0.02mm in resolution and their lengths measured using a ruler with a resolution of 0.5mm.

In equation (1) only the effects of silicon and aluminium contents are considered. But in the widely used non-oriented and grain-oriented silicon-iron steel there are other elements like manganese and cobalt. In some cases the contents of these elements are even higher than that of aluminium or silicon. The standard deviation of the density obtained using equation (1) is of the order of 0.2% to 0.3% [1].

## Determination of sample uniformity

The thickness obtained using the density method is the averaged thickness over a whole sample. Due to variation of the localised thickness the average thickness is different from that at a specified location. To determine the thickness variation two samples from each grade of the samples were selected. Thickness variations in samples were measured on three equally spaced points along their length using the (-ray system. As shown in Table 2 the standard deviation of thickness along the samples is as high as 1 per cent.

(2)

where K is the compensation factor for silicon and aluminium continents, using the (-ray method, and  is obtained in accordance with the data used in practice [37].

# Experimental procedure

Figure 4. Angles between vectors used in calculating magnetisation of single crystals.

As mentioned above a novel saturation magnetisation system was developed that allows high field magnetisation of Epstein size steel samples [18, 19]. As mentioned, Figure 2(a) shows the long air-cored solenoid of this system which was used to measure the saturation magnetisation of the samples tested. Air flux inside the B-coil located at the centre of the solenoid was compensated using a variable mutual inductor. Differential voltage induced in the B-coil is related to the instantaneous magnetic flux density J(t) by Faraday's Law (e(t) = NB AS (dJ(t)/dt)). Where NB is the number of turns of the B-coil and AS is the cross sectional area of the sample to be measured. Magnetised in a heavy ac external magnetic field the waveforms for the external magnetic field magnetisation and induced voltage are shown in Figure 2(b). Following the law of approach to saturation [38] in the region near the peak values of the external magnetic field the sample approaches magnetic saturation JS. The full-wave rectified average of e(t) is given by E = 4 f NB AS JS.

This is measured using the ac function of a 0.1% mean responding multi-meter. Use of the average sensing meter is essential because the distortion levels increase on approaching close to magnetic saturation. The sample also extends entirely though the solenoid and demagnetisation field related to the sample is negligible. The temperature coefficients of expansion of the samples from 20 - 100(C all lie in the range of 11–13 ×10-6/°C [39] and are therefore neglected in the study. The former of the B-coil was made from low thermal expansion material so that the effect of temperature on it is neglected.

# Magnetisation behaviour near saturation

Fallot's study [40] shows that saturation magnetisation of silicon-iron steel is affected by the contents of silicon and aluminium of the steel according to:

(3)

Table 2.

Variation of thickness along some of the Epstein samples tested.

| Silicon content (%) | No. | Thickness (μm) | S.D. (%) |
| --- | --- | --- | --- |
|  |  | Point 1 | Point 2 | Point 3 |  |
| 0.1 | 1 | 648.3 | 644.6 | 639.3 | 0.70 |
|  | 2 | 641.5 | 640.8 | 632.3 | 0.80 |
| 0.2 | 1 | 631.7 | 635.7 | 638.3 | 0.52 |
|  | 2 | 483.1 | 487.0 | 490.8 | 0.79 |
| 0.5 | 1 | 498.8 | 504.4 | 504.4 | 0.65 |
|  | 2 | 486.0 | 491.0 | 493.3 | 0.76 |
| 1.3 | 1 | 481.6 | 478.4 | 474.1 | 0.78 |
|  | 2 | 625.7 | 633.3 | 638.0 | 0.98 |
| 1.8 | 1 | 497.9 | 492.1 | 489.4 | 0.88 |
|  | 2 | 503.4 | 502.0 | 494.3 | 0.98 |
| 3.0 | 1 | 215.0 | 216.0 | 218.3 | 0.77 |
|  | 2 | 284.7 | 285.0 | 280.3 | 0.93 |

Mo in the equation is saturation magnetisation of pure iron. PSi and PAl are the weight percentages of silicon and aluminium contents and KSi and KAl are constants.

Magnetisation at saturation is mainly due to the reversible rotation of domains from their direction of easy magnetisation to the direction of external magnetic field [39]. In a sufficiently large field the magnetisation will reach the saturation value which is the same for all crystallographic directions showing that the individual ionic magnetisation vectors have been rotated so as to be parallel to the applied field. The field needed to fully saturate a silicon-iron steel is normally several hundred kA/m high and requires a huge magnet or a very large power supply to produce the field. However during production of large quantities of silicon-iron strips it is always desirable to substitute the saturation magnetisation in equation (3) with that of a magnetisation produced at a comparatively much lower external field or a so called magnetisation near saturation.

The behaviour of magnetisation near saturation is obtained by considering a specimen of a single crystal subjected to a field H that makes a given angle θ0 with the direction of the easy magnetisation of the crystal  as shown in Figure 4. As H increases the strength of magnetisation of the domain remains unchanged but its direction will deviate from  and approaches H. The angle of deviation ( may be calculated by minimising the total energy composed of crystal anisotropy energy EK and energy of interaction of magnetisation and field . This energy

(4)

is a minimum when  or

(5)

and

(6)

Crystal anisotropy energy of the cubic crystals of the silicon-iron steel is given by:

(7)

The field necessary to magnetise the sample to saturation in the intermediate direction [110] is then [41 - 43]:

(a)                                                                                                      (b)

Figure 5. Influence of depth of saturation on the linear regression of magnetisation. (a) Magnetisation and regressed lines at different exciting field (b) Standard deviation about the regression lines at different excitation fields.

(8)

Anisotropy coefficient  of the crystals of silicon-iron steel is of the order of  [41]. Saturation magnetisation is approximately 2.0 Tesla. So the minimum external field to saturate silicon-iron steel is approximately  HS=50 kA/m. Interaction among domains in polycrystalline silicon-iron steel makes the behaviour of magnetisation near saturation even more complex. Among the extensive list of empirical formulas proposed the equations include logarithmic exponential and arctan functions and use as many as five constants [44].

Measurements on commercial silicon-iron steel show that the law of approach to saturation in either non-oriented or grain-oriented steels can be modelled precisely using Lamont's relation in the external field, H, from 50 kA/m to 200 kA/m.

(9)

C in equation (9) is called the magnetic hardness.

Magnetic hardness for the 0.1-1.8 wt. % silicon non-oriented steel in the finally annealed state is C=799 ± 26 A/m.

Statistical analysis indicates that the standard deviation between the magnetisation measured and that calculated is of the order of 0.09 per cent.

From equations (9) and (3) magnetisation of the non-oriented steel at a given external field  is given by:

(10)

and that of the grain-oriented steel is:

(11)

By comparing equations (10) and (11) it can be seen that with the decrease of external field the magnetisation of non-oriented steel reduces faster than that of the grain-oriented steel.

To estimate the influence of depth of magnetic saturation aluminium content of the non-oriented and grain-oriented steel is assumed zero. Using equations (10) and (11) curves of magnetisation against silicon content are calculated and presented in Figure 5(a). The external magnetic fields in the calculation are chosen Ha = ∞, 200, 100 and 50 kA/m.

Table 3.

Magnetisation near saturation for different branches of the samples (S.D. is standard deviation of the respective measurements).

| Batch No. | Orientation | Nominal silicon Content | Mean Ms Measured at 20° C | No. of Samples in Batch | S.D. of the Mean (%) | S.D. of Original Readings (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Non - oriented | 0.1% | 2.130 | 11 | 0.04 | 0.13 |
| 2 |  |  | 2.131 | 11 | 0.05 | 0.15 |
| 3 |  |  | 2.132 | 11 | 0.06 | 0.21 |
| 4 |  |  | 2.127 | 11 | 0.03 | 0.09 |
| 5 |  |  | 2.128 | 11 | 0.04 | 0.13 |
| 6 |  | 0.2% | 2.123 | 11 | 0.03 | 0.11 |
| 7 |  |  | 2.118 | 11 | 0.02 | 0.06 |
| 8 |  |  | 2.118 | 11 | 0.04 | 0.13 |
| 9 |  |  | 2.122 | 11 | 0.02 | 0.08 |
| 10 |  |  | 2.123 | 11 | 0.02 | 0.07 |
| 11 12 13 14 15 |  | 0.5% | 2.104 | 15 | 0.10 | 0.39 |
|  |  |  | 2.108 | 15 | 0.04 | 0.17 |
|  |  |  | 2.107 | 15 | 0.07 | 0.26 |
|  |  |  | 2.105 | 14 | 0.03 | 0.10 |
|  |  |  | 2.106 | 14 | 0.01 | 0.05 |
| 16 17 18 19 20 |  | 1.3% | 2.079 | 15 | 0.02 | 0.10 |
|  |  |  | 2.077 | 15 | 0.02 | 0.08 |
|  |  |  | 2.073 | 15 | 0.06 | 0.22 |
|  |  |  | 2.075 | 11 | 0.02 | 0.07 |
|  |  |  | 2.075 | 11 | 0.01 | 0.03 |
| 21 22 23 24 25 |  | 1.8% | 2.049 | 15 | 0.01 | 0.05 |
|  |  |  | 2.047 | 15 | 0.03 | 0.12 |
|  |  |  | 2.047 | 15 | 0.04 | 0.15 |
|  |  |  | 2.046 | 15 | 0.01 | 0.04 |
|  |  |  | 2.042 | 15 | 0.01 | 0.05 |
| 26 27 28 29 30 | Grain -oriented | 3% | 2.006 | 23 | 0.03 | 0.13 |
|  |  |  | 2.010 | 23 | 0.02 | 0.11 |
|  |  |  | 2.005 | 23 | 0.02 | 0.09 |
|  |  |  | 2.011 | 23 | 0.03 | 0.16 |
|  |  |  | 2.016 | 23 | 0.02 | 0.08 |

Using linear regression on the data the standard deviation of the regression is found to decrease exponentially with the increase of the external field as shown in Figure 5(b). When external field is higher than 100 kA/m the standard deviation goes down to lower than 0.11%.

Deduced from equation (9) the variation of magnetisation near saturation caused by the variation of external field is given by:

(12)

Under deep saturation the strength of external field is always much bigger than the constant  and therefore the coefficient of equation (12) is much less than unity. Even for the non-oriented steel with a comparatively large constant C = 799 A/m a (20% variation around a peak external magnetic field H = 100 kA/m causes only (0.16% variation in the magnetisation near saturation.

# Dependence of magnetisation near saturation on alloying contents

## Experimental determination of magnetisation near saturation

In the study the peak value of the ac external magnetic field is H=100 kA/m. Sample temperature is maintained at t=20±1°C. In total 440 samples from six different grades of non-oriented and grain-oriented silicon-iron steel were tested. The samples in each grade consist of five branches corresponding to the samples from five original silicon-iron steels of the same nominal silicon content but produced at different periods of time. The number of samples in each branch ranged from eleven to twenty three according to their thickness. Compositions of the samples are analysed using chemical method and their cross-sectional areas determined using the density method as described in section 2.

The influence of thickness variation was reduced by averaging the magnetisation near saturation measured on all samples in each individual branch using:

(13)

(a)                                                                                                 (b)

Figure 6. Regression of magnetisation near saturation against alloying elements. (a) Correlation of magnetisation near saturation measured against that calculated (b) Residual deviation of the regression.

where n is the number of samples in a branch. If the standard deviation of the original measurements is ( then the standard deviation of the mean value of magnetisation of the n measurements would be .

Experiments find that the standard deviations of the original measurements are up to 0.39%. After averaging the standard deviation of the mean values of magnetisation near saturation is found to be less than 0.1%. This is shown in Table 3.

Table 4.

The statistical regression results for silicon and aluminium contents.

|  | Coefficient | Value | Standard deviation | Residual deviation |
| --- | --- | --- | --- | --- |
|  | Intercept | 2.133 | 0.001 | 0.003 (0.14%) |
|  | K1 | 0.0409 | 0.0006 |  |
|  | K2 | 0.0330 | 0.0047 |  |

Nevertheless because of the standard deviation of around 0.2%-0.3% in the determination of the cross-sectional areas using density method [1] the overall standard deviation  for the mean values of magnetisation near saturation of the various branches is approximately as  where  is the maximum standard deviation of the mean magnetisation near saturation in an individual branch.  is that in the determination of cross-sectional areas using density method.

## Regression of magnetisation against alloying contents

Using linear regression the relation between magnetisation near saturation and the contents of silicon and aluminium is obtained as:

JS = 2.133 – 0.0409PS – 0.033PAl	(14)

As shown in Table 4 the standard deviation of the linear regression is in the same order as that of average magnetisation near saturation shown in Table 3.

The correlation between the magnetisation measured and that calculated using equation (14) is shown in Figure 6(a). The suitability of the linear function is further ensured by the normal distribution of standard deviation shown in Figure 6(b).

## The use of conventional density

In the production of large quantities of silicon-iron steels it has been accepted to determine the cross-sectional areas of the samples to use conventional density values instead of the actual densities of the individual samples. Similarly it would be appreciated if a conventional value of magnetisation near saturation could be used to determine the cross-sectional areas of the samples in a grade without introducing too much error. From equation (1) the effect of silicon and aluminium contents on density is:

(15)

(16)

where  is the density of pure iron.

According to equation (14) variation of magnetisation near saturation  caused by the change in the contents of either silicon  or aluminium  are:

(17)

(18)

where  is the magnetisation near saturation of pure iron under regular condition. In the (-ray method variations of the absorption factor K caused by variation of silicon and aluminium contents are given by:

(19)

(20)

Table 5.

Conventional values of magnetisation near saturation density and absorption factor. (Note: Conv. Dens. refers to Conventional density and C.A.F. is to Conventional absorption factor).

|  | Chemical composition |  | Saturation magnetisation method |  | Density method |  | γ-ray method |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Grade | Si (%) | Al (%) |  | Ms (T) | S. D. (%) |  | Conv. Dens. (Kg/m3) | S.D. (%) |  | C.A.F. | S.D. (%) |
| 0.1 | 0.1080 | 0.0370 |  | 2.127 | 0.02 |  | 7854 | 0.01 |  | 1.0023 | 0.02 |
| 0.2 | 0.2202 | 0.0357 |  | 2.123 | 0.03 |  | 7847 | 0.02 |  | 1.0041 | 0.03 |
| 0.5 | 0.4744 | 0.1388 |  | 2.109 | 0.06 |  | 7819 | 0.03 |  | 1.0097 | 0.05 |
| 1.3 | 1.3133 | 0.1402 |  | 2.074 | 0.04 |  | 7764 | 0.02 |  | 1.0230 | 0.03 |
| 1.8 | 1.8074 | 0.3785 |  | 2.046 | 0.06 |  | 7706 | 0.03 |  | 1.0346 | 0.05 |

where K0 = 1.0000 is the absorption factor of pure iron.

Comparing equations (15), (16), (17), (18), (19) and (20), it is found that the influence of silicon on the conventional density method is the least and influence of aluminium is almost the same in all the three methods. From the conventional values and the variation of the silicon and aluminium contents listed in table 1 the conventional values together with the variation of magnetisation near saturation density and absorption factors are calculated for the different grades of steel investigated as presented in Table 5.

## Determination of cross sectional area using saturation magnetisation method

As discussed above at a given temperature and external magnetic field magnetisation near saturation of grades of silicon-iron steel are only determined by their silicon and aluminium contents or the so called the iron dilution factor. On the other hand if saturation magnetisation of silicon-iron steel with known contents of silicon and aluminium is determined under the same condition its cross sectional area can also be determined (from the conventional equation AS = √2Vread/(2π MS NB f ).

For the normal conditions magnetisation near saturation determined from iron dilution factor has a standard deviation of σreg. = 0.14% (=0.003/2.133 ×100%). If the accurate contents of silicon and aluminium are substituted with their respective conventional contents a standard deviation of σconv. ≤ 0.11% as obtained from table 3 will also be added. In this case the total standard deviation for cross-sectional area is determined as:

(21)

which is of the similar order as that of the cross-sectional area determined using the density method [1].

# Conclusion

Unlike all other methods cross-sectional areas determined using saturation magnetisation method represents the magnetically equivalent areas that influence the magnetic behaviour of the samples in practice. Cross-sectional areas determined using saturation magnetisation method is also not affected by the coating of the sample providing an accurate measure of the metal content. An extensive population of different grades of electrical steel samples were tested in order to establish the viability of the technique compared with a well established method normally employed. Under normal conditions (H=100 kA/m t=20° C) the cross-sectional areas determined using the saturation magnetisation method is of the same parity as that of using the conventional density method. The empirical formula obtained is applicable to both non-oriented steels with 0-1.8 wt.% silicon content and grain-oriented steels with 2.8-3.2 wt.% silicon content. To further increase accuracy of the measurements the precision of the original measurement of magnetisation near saturation could be enhanced. The method presented in this paper could be developed to determine similar parameters of other types of ferromagnetic materials such as mild steel bars pipes and other shapes.

Acknowledgment

The author wishes to thank Professor P. Beckley Dr. H. Stanbury and Dr. D. Snell (previously with Orb and European Electrical Steel Newport UK) for help and discussions and preparation of large quantities of samples. The development of the initial system and measurements carried out were mostly the result of dedicated and hard work by Dr. Z. Cao during his postgraduate studies.

References

BS: Magnetic materials - Publication 6404: Part 2 1996 (also - BS EN 60404:13:2007 and IEC-60404-13:2007)

Ball E et al 1987 "Thickness and conductivity measurement of sheets of non-ferrous metals" IEE Proceedings 134 pt. A 10 p 779

Hochschild R 1959 Electromagnetic methods of testing metals Progress in Non destructive Testing Vol. I

Král J et al 2011 Thickness measurement using transient eddy current techniques IEEE Instrumentation and Measurement Technology Conference (I2MTC) 2011

Potanin A S 1988 Contactless sensor to measure the thickness of a ferromagnetic metal strip Measurement Techniques 31 1 pp18-19

Garttiner M et al 1969 Experiments relating to the theory of magnetic direct generation of ultrasound in metals Phys Rev 184 pp 702-704

Dobbs E R 1970 Electromagnetic generation of ultrasonic waves in metals J of the Physics and Chemistry of solids 31 pp 1657-1667

Meredity D J et al 1969 Electromagnetic generation of ultrasonic waves in metals J of the Acoustical Society of America 45 6 pp 1393-1401

Houck J R et al 1967 Direct electromagnetic generation of acoustic waves Physical Review Letters 19 5 pp 224-227

Faulkner W et al 1957 Automatic Process Control with Radiation Gauges IRE Transactions on Production Techniques 2 1 pp 76-81

Yowell R 1992 On-line measurement and control of basis weight and thickness of rubber and plastic web products IEEE Conference Record of Forty-Fourth Annual Conference of Electrical Engineering Problems in the Rubber and Plastics Industries Ohmart Corp Cincinnati OH USA 13-14 April 1992 pp 40-46

Lundahl W N 1948 X-Ray Thickness Gauge for Cold-Rolled Strip Steel Transactions of the American Institute of Electrical Engineers 67 1 pp 83-90

Gottfeld F H and Tidbury D 1954 An X-ray thickness gauge for the measurement of hot-rolled strip steel Journal of the British Institution of Radio Engineers 14 12 pp 622-626

Fumio Tojo et al 2006 Thickness Measurements of Plastic Sheets during the Manufacturing Process: Comparison of Errors with Soft X-ray Thickness and the New Laser Measuring Systems IEEE IMTC 2006 – Instrumentation and Measurement Technology Conference Sorrento Italy 24-27 April 2006 pp 12-15

Canero-Nieto J M et al 2012 Contactless real time measuring system for the length of sheets in stainless steel production lines IEEE (I2MTC) International Instrumentation and Measurement Technology Conference pp 2295-2299

Yamada T et al 1986 Fundamental examination of electromagnetic inductive sensor for testing tube-network National Conference I E C E Japan p 296

Chen J Ma Wet al 2011 Development Of Automatic Iron Loss Measurement System of Magnetic Material With PWM Excitation 2011 IEEE International Conference on Materials for Renewable Energy & Environment (ICMREE) pp 1013-1017

Shirkoohi G H and Cao J Z 1998 Thickness evaluation for steel sheets uses saturation magnetisation Review of Progress in Quantitative Nondestructive Evaluation 17 pp 1501-1508

Beckley P Cao J Z and Shirkoohi G H 1998 Cross section thickness and approach to ferromagnetic saturation IIT (Illinois Institute of Technology) Conference Chicago (May 1998) - unpublished

Mthombeni T and Pillay P 2005 Lamination Core Losses in Motors with Nonsinusoidal Excitation with Particular Reference to PWM and SRM Excitation Waveforms IEEE Trans on Energy Conversion 20 pp 836-843

Kwon S O 2009 Loss Distribution of Three-Phase Induction Motor and BLDC Motor According to Core Materials and Operating IEEE Trans Magn 45 10 pp 4740-4743

Zou L et al 2008 Impact of Saturation Depth Ratio of Iron-Core on the PMFCL International Conference on Electrical Machines and Systems (ICEMS 2008) pp 4338-4343

Wang X and Xie D 2009 Analysis of Induction Motor Using Field-Circuit Coupled Time-Periodic Finite Element Method Taking Account of Hysteresis IEEE Trans Magn 45 3 pp1740-1743

Cheng Z and Takahashi N et al 2010 Effect of Excitation Patterns on Both Iron Loss and Flux in Solid and Laminated Steel Configurations IEEE Trans Magn 46 8 pp 3185

Cheng Z and Takahashi N et al 2009 Analysis and Measurements of Iron Loss and Flux Inside Silicon Steel Laminations IEEE Trans Magn 45 3 pp 1222-1225

Yamaguchi H et al 2008 3D-measurements of magnetic flux on joint regions of SiFe steel model core Journal of Magnetism and Magnetic Materials 320 pp 935–938

Kefalas T D and Kladas A G 2012 Analysis of Transformers Working under Heavily Saturated Conditions in Grid-Connected Renewable Energy Systems IEEE Transactions on Industrial Electronics 59 5 pp 2342-2350

Stumberger G 2010 Prevention of Iron Core Saturation in Multi-Winding Transformers for DC-DC Converters IEEE Trans Magn 46 2 pp 582-585

Klopčič B and Dolinar D et al 2008 Analysis of an inverter-supplied multi-winding transformer with a full wave rectifier at the output Journal of Magnetism and Magnetic Materials 320 pp e929–e934

Dolinar M et al 2006 A Three-Phase Core-Type Transformer Iron Core Model with Included Magnetic Cross Saturation IEEE Trans Magn 42 10 pp 2849-2851

Mork B A et al 2008 Parameter Estimation Methods for Five-Limb Magnetic Core Model" IEEE Trans Power Delivery 23 4 pp 2025-2332

Jaiswal V et al 2006 Accurate Performance Prediction of Three-Phase Induction Motor by FEM Using Separate Saturation Curves for Teeth and Yoke International Conference on Power Electronics Drives and Energy Systems PEDES '06 pp1-4

Shirkoohi G H 1992 Finite element solution of single phase induction machine cores constructed from anisotropic non-oriented steels Journal of Magnetism and Magnetic Materials 112 pp 451-453

Shirkoohi G H 1992 Prediction of improvement in efficiency of induction machines by replacing the core materials using FEM technique Journal of Magnetism and Magnetic Materials 112 pp 416-418

Kim K et al 2011 Characteristics of Ferromagnetic Materials Due to Uneven Magnetic Saturation IEEE Trans Magn 47 10 pp 3669-3672

Zhang C et al 2009 Magnetic characterization of surface-hardened steel Journal of Magnetism and Magnetic Materials 321 pp 3878–3887

Beckley P 1974 Master Standards for Radiation Thickness gauge Sheet Metal industries pp 598-601

Hauser H et al 2006 An approach to modelling the dependence of magnetization on magnetic field in the high field regime Journal of Magnetism and Magnetic Materials 300 pp 273–283

Bozorth R M 1993 Ferromagnetism John Wiley & Sons Ltd ISBN: 9780780310322

Fallot M 1936 Ann Phys 6 p 305

McCurrie R A 1994 Ferromagnetic materials structure and properties Academic Press Ltd ISBN: 0124824951 9780124824959

Shirkoohi G H and Arikat M A M 1994 Anisotropic Properties of High Permeability Grain-oriented3.25% Si-Fe Electrical Steel IEEE Trans Magn 30 pp 928-930

Shirkoohi G H 1996 Anisotropic dependence of magnetostriction in electrical steels under applied linear stress Journal of Magnetism and Magnetic Materials 157/158 pp 516-518

Auwers O V 1934 Magnetic and electrical properties of pure iron and iron containing carbon Gmelin Handbook Inorg Chem 8th Fe Pt A 7 pp 1421-1634

# Footnotes

Manuscript provided by G.H. Shirkoohi, School of Engineering, London South Bank University, 103 Borough Road, London SE1 0AA, United Kingdom; email: maziar.shirkoohi@lsbu.ac.uk. (direct line: +44 (0) 20 7815 7562)

# Text boxes

(a)                                                                                                   (b)

(c)                                                                                                  (d)

(e)                                                                                                   (f)

Figure 3. Variation of alloying contents in individual samples of different grades of electrical steels examined calculated using formula (1):

(a) 0.1% silicon sample; (b) 0.2% silicon sample; (c) 0.5% silicon sample;

(d) 1.3% silicon sample; (e) 1.8% silicon sample; (f) 3.15% silicon sample

(S. D. - standard deviation)

Si

Al

Mn